Electrical design of Brewster window for triple frequency gyrotron

Anil Kumar1, 2, Nitin Kumar1, Udaybir Singh1, Vivek Yadav1, V Vyas2 and AK Sinha1

1Gyrotron Laboratory, Microwave Tube Area

CSIR-Central Electronics Engineering Research Institute (CEERI)

Pilani, Rajasthan, INDIA-333031

2 Department of  Physics, Banasthali University,  Banasthali, Rajasthan, INDIA- 304022

Corresponding author E-mail: anil.gyrotron@gmail.comPh: +91-1596-252229

Abstract: RF window is a critical component of a high power microwave tube and used on the output section of the device for the propagation of RF power. The desired features of an ideal window are minimum return loss, minimum insertion loss, high power handling capability and wide bandwidth. Different dielectric materials such as boron nitride, silicon nitride, sapphire and PACVD diamond are used in a gyrotron RF window. The Brewster window is designed for triple frequency gyrotron and presented in this paper. Brewster window is used in multi frequency gyrotron. Window reflections are the main problem in the design of Brewster window. The transmission band of Brewster window is large and the disk in the window is tilted with a specific angle. Fig 1 shows the schematic view of Brewster window.  Brewster angle and disk thickness are equal to 670 and 1.11 mm, respectively and selected for Brewster window design. Fig. 2 shows the return loss and the insertion loss with wide frequency range for Brewster window.

Fig. 1: Schematic view of the Brewster window

Fig. 2: The return loss and insertion loss with wide frequency range for Brewster window